Q10 KERBS/ EDGES/ CHANNEL/ PAVING ACCESSORIES

115 PRECAST CONCRETE SAFETY KERB

HGV Kerb
A high strength anti-vehicular kerb, specifically designed for busy traffic routes and all urban locations where it is essential to ensure that vehicles remain on the roadway. The profile of the HGV Kerb directs vehicles impacting the kerb back onto the roadway.
Sizes: 
1000 x 415 x 215 (top width) x 310mm (base width)
500 x 415 x 215 (top width) x 310mm (base width)
Finish: Standard
Shades: Grey
Consult with Charcon technical literature for details. Charcon can also provide a design and specification service and it is recommended that they are consulted early in the design process.

115 PRECAST CONCRETE SAFETY KERB:
Manufacturer: Charcon, Hulland Ward, Ashbourne, Derbyshire DE6 3ET. Tel: 01335 372222. Fax: 01335 370074 Web: www.charcon.com 
Product reference: HGV Kerb

Size: 
1000 x 415 x 215 (top width) x 310mm (base width)
500 x 415 x 215 (top width) x 310mm (base width)

Special shapes:
External radius Ref: 36/12 – 958 x 975mm.
External radius Ref: 11/7 – 940 x 975mm.
External radius Ref: 6/4.5 – 916 x 975mm.
External radius Ref: 3 – 802 x 672mm.
External radius Ref: 2 - 441 x 523mm.
External radius Ref: 1.5 – 311 x 392mm.
Internal radius Ref: 36/12 – 958 x 975mm.
Internal radius Ref: 11/7 – 940 x 975mm.
Internal radius Ref: 6/4.5 – 916 x 975mm.
Internal radius Ref: 3 – 802 x 672mm.
Dropper units: 
Type A - 1000 x 415-318 x 215-160mm (Top width).
Type B - 1000 x 318-220 x 160-100mm (Top width HB 2 Profile).
Left hand and right hand versions, types A and B are required to create transition from HGV kerb to British Standard kerb 125mm x 255mm HB 2.
45º Quadrant - 415 x 310mm
60º Quadrant - 415 x 310mm
90º Quadrant - 415 x 310mm.

Finish: Standard

Colour: Grey